Design and Development of Sodium-ion Batteries Based on Layered Transitional Metal Oxide Cathode Material

Zi-Feng Ma

Shanghai Electrochemical Energy Devices Research Center, Department of Chemical Engineering, Shanghai Jiao Tong University, Shanghai, 200240, China

E-mail: zfma@sjtu.edu.cn

The Rechargeable lithium-ion batteries have been considered as a promising power source for the electric vehicles and the grid energy storage systems. However, lithium resources are limited and will restrict the huge applications of lithium-ion batteries. It is of great significance to develop eco-friendly sodium ion batteries which employ abundant sodium resources. Recently, we developed the large-scale synthesis route of NaNi1/3Fe1/3Mn1/3O2 (NFM) by using hydroxide co-precipitation combined with solid-state reaction, and the optimization reaction condition was studied by using in situ XRD. The metastable structure change of NaNi1/3Fe1/3Mn1/3O2 during electrochemical sodium ion intercalation which cycled at 0.1C rate between 2.0 to 4.0V, and 2.0 to 4.3V, were studied by using in operando TXM-XANES and XRD, and the thermal decomposition behavior and structure evolution of charged NaNi1/3Fe1/3Mn1/3O2 cathode material during heating process was measured by using in situ high-energy X-ray diffraction (HEXRD) technique.

References:

[1] Y Xie, H. Wang, G. Xu et. al., Adv. Energy Mater., 2016,6(24) 1601306

[2] H Wang, X.-Z Liao, Y Yang et. al., J.Electrochem. Soc., 163 (2016) A565-A570.

[3] H Wang, X.-Z Liao, Y Xie, et. al., Energy Storage Science and Technology，2016, 5(1):65-68.

Biography

Dr Zi-Feng Ma is currently Chair Professor of Shanghai Jiao Tong University and the founding Director of Shanghai Electrochemical Energy Devices Research Center. He is CIESC Fellow and the Chairman of the Institute of Energy Storage Engineering of Chemical Industry and Engineering Society of China (CIESC).  He was appointed as the Chief Scientist of 973 Program of China for electrochemical energy storage in 2007 and 2013, respectively. He received the Second Prize of the State Scientific and Technological Progress Award and IALB Research Award of the International Automotive Lithium Battery Association in 2018.